Sample Specification Series 1000

Flange adapters shall be used in lieu of

threaded or welded flanges on plain end

ductile and steel pipe. The restraints shall

be manufactured of ductile iron conforming

to ASTM A536. The restraint devices shall be

coated using MEGA-BOND™. (For complete

specifications on MEGA-BOND visit

www.ebaa.com.) The bolt circles and bolt

holes shall conform to ANSI/AWWA

C110/A21.10. The screws shall have a

Rockwell hardness of C40-45 converted

from Brinnell. The flange adapter shall have

a minimum working pressure rating as

shown in the adjacent table. The restraint

shall be the Series 1000 E-Z Flange, as

manufactured by EBAA Iron, Inc., or approved

equal.

All EBAA products intended for installation on ductile iron pipe are designed for and limited to use on ductile iron pipes that comply with the requirements of ANSI/AWWA C151/A21.51 and have a Brinell Hardness or equivalent measurement value that does not exceed 230BHN. These requirements apply to the entire pipe wall profile at all restraining wedge engagement points and to the full penetration depth of each restraining wedge.*

*To learn more about this addendum, please visit: https://ebaa.com/spec/dip